Researcher V. Lapanic

Project 1

Nano-structures for fast-switching and bistable LCD’s.

The severe limitation of nematic liquid crystals in scope for their application in high-speed electro-optical devices is their slow response time (typically higher than 7 ms). Liquid crystal materials possessing ferroelectric properties due to the linearity of the electro-optic effect are characterized by very high speed due to the linearity of the electro-optical effect (in the microsecond range). However, the lack of a stable orientation due to the destruction by even a slight mechanical action is the main obstacle hindering the commercialization of such devices. To solve the above problems we investigated the influence of nano-structures on the dielectric properties and viscosity of liquid crystals, as these parameters have the greatest influence on the threshold and dynamic parameters of different devices based on liquid crystals.

From our experiment we could see that the dielectric spectra of pure nematic composition and composition with the addition of graphene almost identical, except for one effect only. Graphene shifted the frequency of changing the sign of dielectric anisotropy in the smaller region on 100 kHz. If this is right, then studies in this direction are presented prospectively, since the development of compositions with different signs of dielectric anisotropy has been actively involved in many researcher centers due to the synthesis of new classes of compounds. This is also an expensive and lengthy process. In our case, this problem can be solved easier.

The addition of such nano-structures in the nematic matrix reduces the switching time of 1 ms. Adding nano-structures in ferroelectric matrix we reduced switching times 2-2.5 time, and the switching angle increased on 40%, which significantly improves electro-optical characteristics of the LCD. We could prepare samples of LCD without any defects and stable to any mechanical deformation.
It should also be noted that the addition of nano-srtuctures in the ferroelectric compositions led to the effect of the bistability and improvement the alignment condition and resistance of them to mechanical deformation. From the above it can be concluded, nan-structures is promising as an additive to the compositions for development of high-speed and bistable LCD’s.

Fig. 1. Response time for pure LC composition and LC composition with nan-structures.